## Slide 1: Numerical Simulations: Laser Annealed InZnO on Plastic
John Armitage
Cavendish Laboratory: Optoelectronics Group

## Slide 2: Amorphous Oxides: New Student Review
InGaZnO, ZnO, InO, ITO, TiO
Oxides semiconductors are inherently N-type
Possible high mobilities (100 cm2/Vs)
Hosono et. al. – Nature 2004
Notes: I do not know how familiar everyone is with Amorphous Oxides. So, I feel like a brief review is in order. Oxide Semiconductors are a bit odd. Oxides like in most inorganic devices are a insulator. This group of elements with a large delocalized orbitals, end up with overlap between atoms.
Transport it non-band like. Just like organics. Cause of n-type is a little controversial. Oxygen vacancies act as hole traps. Hopping transport. Large delocalized orbitals
How to keep oxide amorphous from becoming crystalline – use different ratios of Zn:Ga:In

## Slide 3: KrF Excimer Laser
248 nm laser
25 ns pulse width

## Slide 4: Results: Laser Annealed Oxides on Silicon
- How is this process occurring? - Can we transfer this process to plastic?
N-Doped Si
Al Electrodes
SiO2
IZO
Low Temp Anneal

## Slide 5: Simulating Laser Annealing
Air
In4ZnO
SiO2
Si
E1R
E1L
E2R
E2L
E3R
E3L
E4R
Step (1): Boundary Conditions
1: EnL+ EnR = E(n+1)L+ E(n+1)
2: d(EnL+ EnR)/dx = d(E(n+1)L+ E(n+1)R)/dx
Step (2): D, H, B
1: D = εE 2: VxE = -dB/dt 3: H = B/μ
Step (3): Absorption rate
1: U = ½ (E·D + E·H) 2: S = E x H
3: dA/dt = -dU/dt - V·S
Step (4): Finite Element – Heat Transfer
1: ϱ*Cp*dT/dt - V·(kVT) = dQ/dt

## Slide 6: Comparison of Simulation to Experimental work
Devices work between 350 mj/cm2 to 550 mj/cm2
Possible Process Window
Temperature cross section of sample at maximum temperature of the IZO layer
Maximum temperature of IZO layer
1) Byskov-Nielsen, et. al. Ultra-short pulse laser ablation of metals: Threshold fluence, incubation coefficient and ablation rates. Appl. Phys. A Mater. Sci. Process. 101, 97–101 (2010).

## Slide 7: Can we cover this process to glass or PEN?
7
Electrodes
Amorphous Oxide
Glass or PEN
Cytop
Al Gate
Glass or PEN
Complete Fabrication
Laser
Determine rough estimate of processing window

## Slide 8: Top Gate Top Contact Glass
Al Electrodes
Amorphous Oxide
Glass
Cytop
Al Gate
Device properties exhibited between 350 mj/cm2 to 550 mj/cm2
Possible Process Window

## Slide 9: Top Gate Top Contact PEN
Al Electrodes
Amorphous Oxide
PEN
Cytop
Al Gate
No working Devices PEN: Max Fluence 100 mj/cm2 – PEN Obliterated at 150 mj/cm2

## Slide 10: Top Gate Bottom Contact
Electrode | Substrate | Electrode Obliteration | Simulated Max Temperature
Au | Glass | 100 mj/cm2 | > 1000C
Au | PEN | 55 mj/cm2 | > 1000C
W | Glass | 45 mj/cm2 | Not Simulated*
W | PEN | 25 mj/cm2 | Not Simulated*
ITO | Glass | 140 mj/cm2 | > 1500C
ITO | PEN | 60 mj/cm2 | > 1000C
Gold, Tungsten and ITO electrodes
Electrodes
Amorphous Oxide
Glass
Cytop
Al Gate
*Tungsten oxidises at 300C.
Electrodes on PEN and Glass Obliterated
Processing Window on Glass: 350 mj/cm2 to 550 mj/cm2
Processing Window on PEN: > 100 mj/cm2
Electrodes
Amorphous Oxide
Glass
Cytop
Al Gate

## Slide 11: Summary
Laser Annealing Amorphous Oxides
  Thermally Insulate the PEN from the IZO layer
  Electrically Insulating UV Absorbent Layer
Stability of N-type Polymers

## Slide 12: Thermally Insulate the PEN
Al Electrodes
Amorphous Oxide
PEN
Cytop
Al Gate
SiO2
- SiO2 thermally protects PEN

## Slide 13: Electrically Neutral UV Absorbent Layer
Electrodes
Amorphous Oxide
PEN
Cytop
Al Gate
TiO2
SiO2

## Slide 14: End
Extra Slides below

## Slide 15: Generating Laser Pulse
X
=
FFT
A few important coefficients

## Slide 16: Simulations of a TiO2 Absorbent Layer
Temperature of Each Layer at 70mj/cm2
With ITO Electrodes
With out ITO Electrodes

## Slide 17: Simulation Parameters
Most parameters can be found online (Er, K, Cp, p, k…)
Extinction Coefficient from UV Vis
Index of refraction from Ellipsometry (n ~= 1.5 )

## Slide 18: ITO Electrodes: TGBC on Glass (Hot Plate)
ITO Electrodes
Amorphous Oxide
Glass
Cytop
Al Gate

## Slide 19: ITO Electrodes: TGBC on Glass and PEN
No working Devices Glass: Max Fluence 125 mj/cm2 – ITO Electrodes Obliterated at 140 mj/cm2 PEN: Max Fluence 55 mj/cm2 – ITO Electrodes Obliterated at 60 mj/cm2
ITO on Glass
ITO on ‘PEN’

## Slide 20: How to Validate the Simulation?
Photo Deflection Spectroscopy built into laser annealing
Laser obliteration typically occurs at melting point of material1.
Melting Point IZO ~= 1900C, Max Temp is 1200C?
1) Byskov-Nielsen, et. al. Ultra-short pulse laser ablation of metals: Threshold fluence, incubation coefficient and ablation rates. Appl. Phys. A Mater. Sci. Process. 101, 97–101 (2010).
Possible Extinction Coefficient Increase During Laser Annealing